## Slide 1: Measurement of formation cross-sections and decay properties for short-lived isomers produced in photonuclear interactions
CSIRO MINERAL RESOURCES
Justin Delaney | CSIRO & University of Wollongong Dr Chanel Tissot | CSIRO
Dr James Tickner | Chrysos

## Slide 2: What is GAA?
CSIRO has been developing various mineral assay techniques, such as Gamma Activation Analysis (GAA) for several years.
Commercialised by Chrysos Corporation as PhotonAssay.
Primarily aimed at detection of gold and other precious metals.

## Slide 3: How many elements can we measure?

## Slide 4
Non-destructive
    No sample preparation required. Original sample can be preserved
Real time
    Results can be obtained in seconds/minutes
Highly sensitive
    Can measure concentrations << 1ppm
    Can measure bulk samples, unlike x-ray techniques (XRD,XRF…)
Can be used “in the field”
    Possible to deploy a complete GAA system to a mine or other industrial facility
    Doesn’t require a reactor, like NAA
Advantages of GAA

## Slide 5
Several nuclear reactions can lead to the production of isomers;
Important nuclear interactions
σ ≈ 0-10 mb
σ ≈ 10-100 mb
σ ≈ 0.1-400 b

## Slide 6: Existing literature
Number of data sets: 154
36
0
Images taken from EXFOR database: https://www-nds.iaea.org/exfor/exfor.htm

## Slide 7: Experimental details
Results collected with a high-purity germanium detector (HPGe)
1kW electron accelerator used as bremsstrahlung source.
Could not irradiate and measure simultaneously. Used pneumatics to rapidly move sample between linac beamline and detector station.
Measurements conducted in 0.5 MeV intervals, over 6.5 – 10.5 MeV range.
Ir
ZnSe
KBr
Y
Au
Hf

## Slide 8: Decay properties
Includes half-life, gamma emission energies & probabilities, among others.
Quality of existing data is poor in some areas.
(207.5 ± 0.1) keV
(110.3 ± 1.2) keV
43.7 keV (13.9 ± 1.4)% 44.5 keV (24.7 ± 2.4)%

## Slide 9: Decay properties
Isomer | Half life (s) | Existing emission energy (keV) | Revised emission energy (keV) | Emission probability (%) | Revised emission probability (%)
Au197m | 7.73 | 279.01 (5) | 279.0030 (12) | 70.9 | -
Br79m | 4.86 | 207.5 (1) | 207.4791 (12) | 76.3 (3) | -
Cd111m | 2912 | 150.825 (15) 245.395 (20) | - - | 29.1 (18) 94 (7) | 
Hg199m | 2560 | 68.894 70.818 158.3 (1) 374.1 (1) | - - 158.4053 (12) 373.9027 (12) | 17.7 (11) 29.8 (19) 52.3 13.8 (11) | -
Pd107m | 21.3 | 214.6 (3) | 214.4972 (12) | 68.7 | -
Tb158m | 10.70 | 43.744 44.482 110.3 (12) | - - 109.7845 (12) | 13.9 (14) 24.7 (24) 0.92 (3) | 13.46 21.41 -
W183m | 5.2 | 57.981 59.318 | - - | 36.3 (10) 62.3 (16) | 37.15 62.77

## Slide 10: Formation cross-sections
How to measure them?
can be simulated
can be calculated
can be measured

## Slide 11: Formation cross-sections
How to extract the cross section?
Penfold-Leiss Unfolding1:
Produces non-physical solutions.
Why?
- Requires high precision results
- Assumes monoenergetic electron beam
1. Penfold, A. & Leiss, J., Phys Rev, 114, 5, Analysis of Photonuclear Cross Sections, (1959)
How to extract the cross section?
Cook’s Least Structure Solution2:
- Generate several random vectors “
- Calculate χ2 statistic to find acceptable solutions
- Find solution with smallest “structure function”, ie, the smoothest curve
2. Cook, B., Nuc. Inst. & Meth., 24, 256-268, Least Structure Solution of Photonuclear Yield Functions (1963)

## Slide 12: Potential limitations
Experimental uncertainties
    Linac operating parameters
    (γ,n) contributions
    (n,γ) contributions
Interference from other elements
    Activation of shielding
    Photofission of U and/or Th
High spin differences
    Isomers with large spin differences (ΔJ > 6) between excited and ground states are difficult to activate. Only 2 cases have been documented to date3,4
3. Belov, A.G. et al, Hyperfine Interact., 107, 167-173, Excitation of the high-spin 180Hf isomer and de-excitation of the 180Ta isomer in (γ,γ) reactions (1997) 4. Tickner, J., Appl. Rad. & Iso., 110, 42-46, Photoexcitation of the high-spin J=8 isomer in 176Yb using 8.5 MeV end-point energy bremsstrahlung (2016)
Mn56

## Slide 13: Applying GAA to industry
Recently commercialised by Chrysos Corporation as PhotonAssay.
Practical applications for real-time quality control in mining.
Gold industry alone produces >$US100 billion per year.

## Slide 14: Future Work
Catalogue unmeasured (γ,γ) cross-sections.
Quantify photofission product yields for 238U and 232Th.

## Slide 15: Thank you
  Justin Delaney PhD Candidate
    T +61 2 9710 6777
    E justin.delaney@csiro.au
    W www.csiro.au
CSIRO Mineral resources